VANGUARD™ VERTICAL PRIVACY FENCE

SPECIFICATIONS

ALUMINUM FENCE

PART 1 GENERAL

1.01 WORK INCLUDED

The contractor shall furnish and install the fences listed.

1.02 SYSTEM DESCRIPTION

Fence system shall be Vanguard™ Vertical Privacy Fence

1.03 QUALITY ASSURANCE

Laborers  and supervisors involved with the installation of the fence will be experienced with all aspects of the construction process.

1.04 REFERENCES

ASTM B117 – Practice for Operating Salt Spray Equipment

ASTM B221 – Standard Specifications for Aluminum and Aluminum-Alloy Extruded Bars , Rods, Wire, Profiles and Tubes.

ASTM D523-89 -  Test Method  for Specular Gloss.

ASTM D2244 – Test Method for Calculation of Color Differences From Instrumentally Measured Color Coordinates

ASTM D2247 – Test Method for Humidity

ASTM D2794 – Test Method for resistance of Organic Coatings to the effects of Rapid deformation (Impact Resistance)

ASTM D3359–95A - Test Method for Measuring Adhesion By Tape Test

1.05 SUBMITTAL

Manufactures  detail drawings of fences shall be submitted for approval prior to the installation.

PART 2 MATERIALS

2.01 MANUFACTURER

The fencing will be as manufactured by AMERICAN FENCE SYSTEMS, INC., South Plainfield, NJ. Fence will be manufactured in the STYLE Vertical Privacy Fence

2.02 MATERIALS

Pickets, Posts and Rails shall be manufactured to conform to requirements as specified in ASTM B221. Rails,Tubular  Pickets shall be Alloy 6063-T6. Posts shall be Alloy 6105-T5

Pickets shall be 7/8” x 4” Tongue and Groove with a wall thickness of .063”. Rails shall be 2.00” x 3.00” channel with a total wall thickness of .094”. The u-channels at the ends of the sections shall be 1” x 7/8”  with a wall thickness of .062”. Posts shall be 3.00” square with a .125” wall thickness. Gate Post shall be 4” with a .125” wall thickness.

Aluminum castings shall be used for caps and wall mounts.

Gate hardware suitable for the proper operation of gates will be included with gates.

2.03  ASSEMBLY

Pickets will be inserted into top and bottom horizontal rails to create the privacy panel. The rails will be secured to the posts with painted stainless steel screws.

Gates will be fabricated to match fence. The gate horizontal rails will be welded to a 2 1/2” gate uprite with a wall thickness of 0.125”.

2.03 COATING

All Vanguard components are cleaned and prepared by using a state of the art no rinse dry-in place coating which is an environmentally-friendly, patented pretreatment that provides results equal to chrome without the environmental concerns.   Vanguard’ pretreatment is not EPA listed nor does it contain any restricted Heavy Metals. Vanguard pretreatment is approved in Europe by GSB and Qualicoat.  Once pretreated, a Super Durable Polyester TGIC Powder coating is applied electro-statically to the pretreated substrate and cured by using both IR and Gas Convection.  The resulting Vanguard finish meets or exceeds all of the testing requirements of the AAMA 2604-98 specification to provide a superior coating finish with exceptional weathering and corrosion properties

2.04 Coating Performance

RESULT

Adhesion		D3359-95A	5b100% No Creepage

Impact resistance	D2794-93		Up to 160 in. lbs.

> 1/10” Deformation

Hummidity	D2247		3000 Hrs. No Effect

Salt Spray		B117		Scribe Rating 8

Blister Rating 10

Weathering	D2244		5 Year South Florida Sun

PART 3 – EXECUTION

3.01 PREPARATION

Contractor will layout fence according to plans.

3.02 Installation

Installation should be performed using standard industry practices.